# WebApp vs LAMMPS Validation for Co25Cr25Fe0Mn25Ni25 Alloy

Comparison of WebApp predicted parameters with LAMMPS/formula-based verification for Fe = 0 at.% composition (Co25Cr25Fe0Mn25Ni25).

| Parameter | WebApp predicted value | LAMMPS verified value |
| --- | --- | --- |
| ΔHmix (kJ/mol) | -4.886 | -4.651 (FCC reference) |
| Delta Radius (%) | 1.818 | 1.818 |
| Mean Atomic Radius (pm) | 137.5 | 137.5 |
| Density (g/cm³) | 8.052 | 8.079 |
| Mean Melting Point (K) | 1798.9 | — |
| VEC | 8.00 | 8.00 |
| Mixing Entropy (Sconf/R) | 1.386 | 1.386 |
| Lambda | 0.419 | 0.419 |
| Omega | 4.244 | — |
| FCC phase stability temperature | — | 1273–2073 K range from heating/quenching analysis |

## Manuscript Validation Table Format

| Alloy | WebApp predicted data | LAMMPS / Formula verified data |
| --- | --- | --- |
| Co25Cr25Fe0Mn25Ni25 | ΔHmix −4.886 kJ/mol; δ 1.818%; Mean atomic radius 137.5 pm; Density 8.052 g/cm³; Mean melting point 1798.9 K; VEC 8.00; Ω 4.244 | ΔHmix −4.651 kJ/mol (FCC reference); Density 8.079 g/cm³; VEC 8.00; δ 1.818%; FCC structure verified through LAMMPS heating/quenching |

Similarity: Excellent agreement; density difference ≈0.33%; structural descriptors closely matched.