# LAMMPS and Machine Learning Prediction Verification Report

System: Fe35Ni5CoCrMn20 High Entropy Alloy (FCC structure)
Purpose: Comparison of ML/webapp predicted physicochemical parameters with LAMMPS relaxed structure verification and formula-based calculations.

## Figure Description

Figure 1 presents the OVITO visualization of the FCC Fe35Ni5CoCrMn20 alloy structure before and after thermal/quenching treatment. The initial structure shows a highly ordered FCC arrangement with uniform atomic distribution. After simulation, the structure exhibits atomic rearrangement and local structural distortion caused by thermal relaxation and energy minimization.

The radial distribution function (RDF) obtained from OVITO confirms the change from a sharp crystalline FCC structure to a relaxed atomic configuration. The reduction and broadening of RDF peaks indicate local atomic disorder while maintaining the dominant FCC-based structure.

Figure 2 shows the LAMMPS relaxed FCC structure analysis. The final minimized system contains 5760 atoms, with a relaxed density of 7.873 g cm⁻³. The minimized potential energy and atomic arrangement were used for verification of thermodynamic parameters.

## Table 1. Comparison Between ML Prediction and LAMMPS/Formula Verification

| Parameter | Webapp (ML) Value | LAMMPS / Formula Verified Value |
| --- | --- | --- |
| Mixing enthalpy, ΔHmix (kJ mol⁻¹) | -2.609 | -2.558 (LAMMPS FCC reference calculation) |
| Atomic size difference, δ (%) | 1.560 | 1.560 (Formula calculation) |
| Lambda parameter, Λ | 0.609 | 0.609 (Formula calculation) |
| Mean atomic radius (pm) | 138.75 | 138.75 (Composition-weighted formula) |
| Density (g cm⁻³) | 7.862 | 7.873 (LAMMPS relaxed FCC structure) |
| Mean melting temperature, Tm (K) | 1813.8 | 1813.8 (Composition-weighted formula) |
| Configurational entropy, Sconf/R | 1.483 | 1.483 (−Σci ln(ci)) |
| Omega parameter, Ω | 8.572 | 8.742 (Calculated using LAMMPS ΔHmix + entropy) |
| Valence electron concentration (VEC) | 7.70 | 7.70 (Composition-weighted formula) |

## LAMMPS Verification Summary

LAMMPS relaxation produced a final FCC structure containing 5760 atoms. The relaxed potential energy per atom was -3.999269 eV atom⁻¹ and the final density was 7.873 g cm⁻³. These values were used for verification of the thermodynamic descriptors.